PC/ABS AC1260

Source  Water bucket, lampshade   ，

Application   TV front frame

Performance table

|  | Testing standards |  |
| --- | --- | --- |
| Melt Flow Index | ASTM D1238 | 20 g/10min |
| Tensile strength | ASTM D638 | 60MPa |
| Elongation | ASTM D638 | 8% |
| Bending strength | ASTM D790 | 90MPa |
| Bending modulus | ASTM D790 | 2500MPa |
| Notched IZOD Impact | ASTM D256 | 150J/M |
| Density | ASTM D792 | 1.26g/cm3 |
| FR | UL94 | 1.6MM V0 |