PC-20NP

Source   Sheet、Headlight Shell、CD     ，Application    Automotive

Performance table

|  | Testing standards |  |
| --- | --- | --- |
| Melt Flow Index | ASTM D1238 | 17-21 g/10min |
| Tensile strength | ASTM D638 | 60 MPa |
| Elongation | ASTM D638 | 90 % |
| Bending strength | ASTM D790 | 88 MPa |
| Bending modulus | ASTM D790 | 2150 MPa |
| Notched IZOD Impact | ASTM D256 | 500 J/m |
| Density | ASTM D256 | 1.19g/cm3 |