PC/ABS Flame retardant / anti-static

Source  lampshade、Instrument panel cover、CD       ，

Application    Electronics

Performance table

|  | Testing standards |  |
| --- | --- | --- |
| Melt Flow Index | ASTM D1238 | 5 g/10min |
| Tensile strength | ASTM D638 | 60MPa |
| Elongation | ASTM D638 | 10% |
| Bending strength | ASTM D790 | 85MPa |
| Bending modulus | ASTM D790 | 2600MPa |
| Notched IZOD Impact | ASTM D256 | 300J/M |
| Density | ASTM D792 | 1.21g/cm3 |
| FR | UL94 | 3.0MM V0 |