PC/ABS SRR-VA80

Source  lampshade、Instrument panel cover、CD       ，

Application    Household appliances

Performance table

|  | Testing standards |  |
| --- | --- | --- |
| Melt Flow Index | ASTM D1238 | 50 g/10min |
| Tensile strength | ASTM D638 | 60MPa |
| Elongation | ASTM D638 | 15% |
| Bending strength | ASTM D790 | 80MPa |
| Bending modulus | ASTM D790 | 2300MPa |
| Notched IZOD Impact | ASTM D256 | 350J/M |
| Density | ASTM D792 | 1.18g/cm3 |
| FR | UL94 | 2.0MM，5VB |